## Slide 1: Simulation of CFRP elements heated by moving laser heat source in Abaqus
Suba Siva Chandran, Kalimuthu, 28.05.2021

## Slide 2: Simulation of CFRP elements heated by moving laser heat source in Abaqus
25
25
Moving laser heat source
Traversing
path
2
Resin (0.001 mm)
 | Density (ton/mm3) | Sp.heat (mJ/ton K) | Conductivity (mW/mm2K)
Thermoset resin | 1,30e-9 | 1,1e9 | 2,5e-1
Fiber | 1,60e-9 | 9,50e8 | 4,5 (longitudinal) 0,67 (transverse)
Moving laser heat source is implemented in ABAQUS by FORTRAN subroutine DFLUX
Gaussian model describing the laser beam heat source is implemented based on research article “Application of Abaqus to analysis of the temperature field in elements heated by moving heat sources”
Material properties used:
Simulation model setup

## Slide 3: Simulation of CFRP elements heated by moving laser heat source in Abaqus
 | 1 micrometer | 10 micrometers | 50 micrometers
Thermoset resin | 508,103 | 446,628 | 435,75
CFRP | 508,104 | 446,929 | 441,693
Steps carried out based on discussion from previous meeting:
  Thermal conductivity was changed
  Material parameters were checked
  Connections of the parts and material orientations were checked
  Temperature difference was studied based on the resin thickness
Thermal conductivity with same values are applied in both directions
Temperature differences based on resin thickness
k11 | k22 | k33
4,5 | 0,67 | 0,67

## Slide 4: Simulation of CFRP elements heated by moving laser heat source in Abaqus
Steps carried out based on discussion from previous meeting:
  Mesh is refined in the centre region where the heat source traverses through
  Free convection from the model based on film coefficients
  Increment size changed from 0.1 to 0.001
  Temperature values were measured at same points for all the simulations
Geometry
a = 220.3 mm, b = 220.3 mm

## Slide 5: Temperature values of Simulation attempts
 | 1 micrometer | 10 micrometers | 50 micrometers
Thermoset resin | 400,895 | 390,21 | 340,328
CFRP | 400,9 | 390,632 | 350,75
Temperature values based on Increment size – 0.001 alone
 | 1 micrometer | 10 micrometers | 50 micrometers
Thermoset resin | 411,17 | 400,313 | 351,67
CFRP | 411,376 | 402,687 | 369,446
 | 1 micrometer | 10 micrometers | 50 micrometers
Thermoset resin | 392,008 | 380,484 | 329,411
CFRP | 392,18 | 382,502 | 345,461
Temperature values based on free convection and Increment size – 0.001
Temperature values based on free convection and Increment size – 0.1

## Slide 6: Temperature values of Simulation (New material props) – 28.05.2021
Inc size: 0.1
Inc size: 0.01

## Slide 7: Temperature values of Simulation (New material props) – 02.06.2021
Inc size: 0.1
Inc size: 0.01
Inc size: 0.001

## Slide 8: Temperature values of Simulation (New material props) – 28.05.2021
 | 1 micrometer | 10 micrometers | 50 micrometers
Thermoset resin | 336,256 | 328,349 | 291,763
CFRP | 336,363 | 329,614 | 302,454
 | 1 micrometer | 10 micrometers | 50 micrometers
Thermoset resin | 370,653 | 363,186 | 326,703
CFRP | 370,799 | 364,956 | 339,02
Temperature values based on free convection and Increment size – 0.01
Temperature values based on free convection and Increment size – 0.1

## Slide 9: Temperature values of Simulation (New material props) – 02.06.2021
All the below values in the table correspond to 50 micrometers at different increments such as 0.1,0.01 and 0.001 respectively
 | 0.1 | 0.01 | 0.001
Thermoset resin | 291,763 | 326,703 | 330,702
CFRP | 302,454 | 339,02 | 343,859

## Slide 10: Temperature values of Simulation (1st Setup) – 05.07.2021
 | 1 micrometer | 10 micrometers
Thermoset resin | 314,988 | 310,508
CFRP | 315,088 | 311,778

## Slide 11: Temperature values of Simulation (2nd Setup) – 05.07.2021
 | 1 micrometer | 10 micrometers
Thermoset resin | 251,078 | 233,313
CFRP | 251,23 | 237,051

## Slide 12: Simulation with Gauss profile (d = 4mm) – 01.08.2021
 | 1 micrometer | 10 micrometers
Thermoset resin | 505,827 | 492,241
CFRP | 506,098 | 496,651

## Slide 13: Simulation without Gaussian profile (d = 3.6 mm) – 01.08.2021
 | 1 micrometer | 10 micrometers
Thermoset resin | 351,827 | 346,458
CFRP | 351,96 | 348,103